METHACRYLATE-FUNCTIONALIZED COVERSLIPS

Last updated 2/4/2013 by W.H.

Materials

# Sulfuric Acid (H2SO4)**				3-(Trimethoxysilyl)propyl methacrylate

Hydrogen Peroxide (H2O2)**			200 proof ethanol

Glass coverslips, or glass-bottomed 96-well plate

Methods

- Treat coverslips with Piranha (25% H2SO4, 15% H2O2) for 1 hour on an orbital shaker.  Piranha is highly toxic!  Make solution in the hood and make sure to dispose of it safely. **In lieu of Piranha treatment, treatment with oxygen plasma is preferred if the equipment is available. We typically treat glass surfaces for ~10 minutes at high RF power with the pressure under 500. Then skip to step #5.

- Sonicate coverslips while in piranha for 15min.

- Rinse coverslips thoroughly with H2O and EtOH.

- Dry coverslips under nitrogen.

- Prepare 100 mL of 95% ethanol adjusted to pH 5.0 with glacial acetic acid, then add 3-(Trimethoxysilyl)propyl methacrylate to 2% v/v.

- Submerge cover slips in this solution, or if treating a 96-well plate, add 100 µl/well. Shake for 2 minutes.

- Remove solution and thoroughly wash coverslips or wells with 200 proof ethanol 3x.

- Shake off excess ethanol and dry at 120C for 20 minutes if using coverslips. If using 96-well plates, dry at 40C for 30-40 minutes so as to not melt the plastic well sides.

- Store coverslips or plates in dessicator wrapped in foil.